UNITED STATES DEPARTMENT OF THE INTERIOR

GEOLOGICAL SURVEY

Gold and spectrographic analyses of 110 outcrop and 238

B-horizon soil samples from the western Vermilion district,

northeastern Minnesota

By

J.B. McHugh, R.T. Hopkins, H.V. Alminas, and G.T. Hill

Open-File Report 92-XXX

This report is preliminary and has not been reviewed for conformity

with U.S. Geological Survey editorial standards or with the North

American Stratigraphic Code.  Any use of trade, product or firm

names is for descriptive purposes only and does not imply

endorsement by the U.S. Government.

1992

CONTENTS

Page

Introduction................................................ 1

Sample Collection............................................1

Sample Preparation...........................................1

Analytical Procedures....................................... 2

References Cited............................................ 3

TABLES

Table 1.  Gold and spectrographic analyses

of 110 outcrop samples from the west

Vermilion district, northeastern

Minnesota.........................................

Table 2.  Gold and spectrographic analyses

of 238 B-horizon soil samples from the west

Vermilion district, northeastern

Minnesota........................................

INTRODUCTION

The study area within the west Vermilion district, as

referred  to in this report, encompasses some 428 km2. It is a

westward extension of an area described in U.S. Geological Survey

Bulletin 1984 (Alminas and others, 1992).  The silver and base-

metal data for the eastern study area is listed in U.S.

Geological Survey Open-File Report 81-999 (Grimes and others,

1981) and the gold data is listed in U.S. Geological Survey Open-

File 90-86 (McHugh and others, 1990).

The greenstone belt is composed of mafic metavolcanic and

associated rocks that are intruded on both the north and south by

major granitoid bodies.  These rocks have mineral assemblages

characteristic of the greenschist-facies metamorphism.  The

general geology of the district has been described by Sims

(1976).  Pleistocene glacial materials consisting of till,

outwash and lacustrine deposits, associated with the Wisconsin

episode of glaciation, cover the area.  These are the parent

materials of the B-horizon soils sampled here.

The field work was completed in June of 1991.

SAMPLE COLLECTION

B-horizon soil samples were collected at 238 localities

along roads, rivers and lake shores.  Outcrop samples were

collected at 110 of these sites (within 6.7 m of the soil site)

and have the same latitudinal and longitudinal parameters as the

corresponding soils.   The B-horizon soil samples were collected

at a depth of 30 to 45 cm.  Although variable from site to site,

these soils are generally fine to medium grained with a low to

moderate organic content and range in color from yellow through

red to light brown.  Characteristically the B-horizon soils

contain higher concentrations of Fe and Mn oxides than A-horizon

soils, have a substantially lower organic content, and are

coarser with  a greater content of fragmental rock material .

Outcrop samples were collected as composited chip samples

and generally incorporated substantial weathered surface

material.

SAMPLE PREPARATION

The soil samples were air-dried in the original cloth sample

bag.  Extremely clay-rich samples were disaggregated in a jaw

crusher, using a wide jaw setting.  All of the soils were then

sieved through an 80-mesh (177-�m opening) sieve, and a 84-g

(3-oz) container of the fine fraction was saved for analysis.

Outcrop samples were crushed in a jaw crusher and ground in

a vertical grinder to approximately 105 �m.

1

ANALYTICAL METHODS

Each sample was analyzed for 35 elements using a

semiquantitative direct-current arc emission spectrographic

method (Grimes and Marranzino, 1968).  Spectrographic results

were obtained by visual comparison of spectra derived from the

sample against spectra obtained from standards made from pure

oxides and carbonates.  Standard concentrations are geometrically

spaced over any given order of magnitude of concentrations as

follows:  100, 50, 20, 10 and so forth.  Samples whose

concentrations are estimated to fall between those values are

assigned values of 70, 30, 15, and so forth.  The precision of

the analytical method has been determined to be within one

reporting interval 83 percent of the time and within two

reporting intervals 96 percent of the time (Motooka and Grimes,

1976).

The gold content of the outcrop and soil samples was

determined using an atomic-absorption spectrophotometric method

described below:

A 5-gm sample is roasted for 1 hour at 680o C.  Gold is then

extracted with a hydrobromic acid- 0.5 bromine solution and MIBK

(methyl isobutyl ketone).  Electrothermal atomic-absorption

spectroscopy, using background correction, is used to determine

gold to 0.001 ppm (1 ppb) (O'Leary and Meier, 1986).

2

REFERENCES CITED

Alminas, H.V., McHugh, J.B., and Perry, E.C.Jr., 1992,  Precious-

and Base-Metal Mineralization in the West-Central Vermilion

District, Portions of St.Louis, Lake, and Cook Counties,

Northeastern Minnesota:  U.S. Geological Survey Bulletin

1984 37 p.

Grimes, D.J., and Alminas, H.V., 1981,  Analyses of A-horizon

soil and outcrop samples from the Vermilion district,

northeastern   Minnesota:  U.S. Geological Survey Open-File

Report 81-999 36 p.

Grimes, D.J., and Marranzino, A.P., 1968, Direct-current arc and

alternating-current arc spark emission spectrographic field

methods for the semiquantitative analysis of geologic

materials:  U.S. Geological Survey Circular 591, 6 p.

McHugh, J.B., Alminas, H.V., and Perry, E.C.Jr., 1990,  Gold

contents of 766 A-horizon soil samples from the Vermilion

District, northeastern Minnesota: U.S. Geological Survey

Open-File Report 90-86, 20 p.

Motooka, J.M., and Grimes, D.J., 1976,  Analytical precision of

one-sixth order semiquantitative spectrographic analyses:

U.S. Geological Survey Circular 738, 25 p.

O'Leary, R.M., and Meier, A.L., 1986, Analytical Methods used in

Geochemical E.exploration, 1984: U.S. Geological Survey

Circular 948, 48 p.

Sims, P.K., 1976, Early Precambrian tectonic-igneous evolution in

the Vermilion district, northeastern Minnesota:  Geological

Society of America Bulletin v. 87, p.379-389.

3