Table  2. Comparison of preparation and analytical procedures used for solid samples by ALS Chemex and Frontier Geosciences laboratories

|  | ALS Chemex | Frontier Geosciences |
| --- | --- | --- |
| Step (in sequence) |  |  |
| (1) Dry | 60°C | — |
| (2) Fine crush | Entire sample | — |
| (3) Remove split | 250 g | 0.5g |
| (4) Pulverize | To >85% <75 | — |
| (5) Digest/leach | HF-HNO3-HClO4-HCl | Aqua regia (HCl-HNO3) |
| (6) Analysis* | CVAA | CVAFS |

*Mercury detection method only.  The same chemical procedure for extraction of mercury from solid samples is used by both laboratories.